Ceramics Sciences Corporation

57-101 Copper Conductor on Aluminum Nitride
Copper




> 98% pure copper
Substrate




Ceramics Sciences AlN
Substrate thickness


>0.025”
Bonding mechanism


Reaction bonding
Copper thickness



up to 100 microns
Metallized area



up to 4” x 4 ’’
Minimum width of conductor lines   150 microns
Minimum spacing


150 microns
Insulation resistivity


1013 ohm-cm
Conductor resistivity


2-5 miliohm/sq
Dielectric strength


>15kV / mm
Adhesion strength


>25 N (initial)






>20 N (aged 48h @ 150 C)

Solderability
Excellent, solder tinning or bumping 
Thermal cycling



>200 cycles for 2” X 2” X .04”

------------------------------------------------------------------------------------------------------------Visit our website at: http://www.cearmicsciencescopr.com
The information given here is based on data deemed to be reliable, but Ceramics Sciences makes on warranties as to the accuracy and assumes no liability arising out of its use by others. 

