                                                     Ceramics Sciences Corporation

CS5360 Conductor Composition

	Table 1

Typical Fired properties

	Resistivity (mΩ/sq)               <6
(12 µ fired thickness)

Thickness                      up to 20 µ 



Product Description

CS5360 is a gold conductor that fires at low temperatures.  It is suitable for variety substrates that require low temperature (<650 C) 

processing. 
Processing Conditions

Printing

325 mesh stainless screen with a 12.5 micron emulsion.   
	Table 2

Properties Relevant to Processing

	Viscosity (Pa s)                    250-350

(Brookfield HBT #14 spindle, @10 rpm, 25C)
Solids                                  90 +/- 1.5

Coverage                              60 cm2/g




Drying and Firing
Allow prints to level for 3-4 minutes at room temperature, and then dry at 150 C in air for 5-10 minutes.

Firing is accomplished at 525-650 C peak for 5-8 minutes in air.  Overall firing cycle may be 30 or 0 minutes.


------------------------------------------------------------------------------------------------------------Visit our website at: http://www.cearmicsciencescopr.com
The information given here is based on data deemed to be reliable, but Ceramics Sciences makes on warranties as to the accuracy and assumes no liability arising out of its use by others. 

